Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/08 18:55:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_8wks_A_1 |  |  |  |  |  |  | Calculation date and time | 2023/11/09 10:05:26 |
| Database name | SMF run-2023-11-08.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2418 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 12 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 6,358 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.733 | 0.472 | 86,113 |  |  | Mw | 11,052 |
| Peak top | 11.265 | 41.798 | 7,600 |  |  | Mz | 18,008 |
| Peak end | 11.832 | 34.556 | 2,016 |  |  | Mz+1 | 25,589 |
|  |  |  |  |  |  | Mv | 11,052 |
| Height [mV] | 40.823 |  |  |  |  | Mp | 9,989 |
| Area [mV*s] | 2795.497 |  |  |  |  | Mz/Mw | 1.629 |
| Area% [%] | 59.017 |  |  |  |  | Mw/Mn | 1.738 |
| [eta] | 11051.52598 |  |  |  |  | Mz+1/Mw | 2.315 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 376 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.832 | 34.556 | 2,016 |  |  | Mw | 727 |
| Peak top | 12.232 | 51.952 | 583 |  |  | Mz | 1,082 |
| Peak end | 12.955 | 1.529 | 25 |  |  | Mz+1 | 1,336 |
|  |  |  |  |  |  | Mv | 727 |
| Height [mV] | 50.660 |  |  |  |  | Mp | 659 |
| Area [mV*s] | 1941.289 |  |  |  |  | Mz/Mw | 1.487 |
| Area% [%] | 40.983 |  |  |  |  | Mw/Mn | 1.936 |
| [eta] | 727.41813 |  |  |  |  | Mz+1/Mw | 1.837 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 845 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.733 | 0.472 | 86,113 |  |  | Mw | 6,820 |
| Peak top | 12.232 | 51.952 | 583 |  |  | Mz | 17,268 |
| Peak end | 12.955 | 1.529 | 25 |  |  | Mz+1 | 25,522 |
|  |  |  |  |  |  | Mv | 6,820 |
| Height [mV] | 91.484 |  |  |  |  | Mp | 9,989 |
| Area [mV*s] | 4736.786 |  |  |  |  | Mz/Mw | 2.532 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 8.071 |
| [eta] | 6820.37085 |  |  |  |  | Mz+1/Mw | 3.742 |