Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/08 19:15:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_8wks_A_2 |  |  |  |  |  |  | Calculation date and time | 2023/11/09 10:05:42 |
| Database name | SMF run-2023-11-08.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2419 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 13 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 5,952 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.748 | 0.044 | 84,214 |  |  | Mw | 10,748 |
| Peak top | 11.262 | 48.921 | 7,651 |  |  | Mz | 17,814 |
| Peak end | 11.877 | 39.031 | 1,779 |  |  | Mz+1 | 25,439 |
|  |  |  |  |  |  | Mv | 10,748 |
| Height [mV] | 48.062 |  |  |  |  | Mp | 9,927 |
| Area [mV*s] | 3360.676 |  |  |  |  | Mz/Mw | 1.657 |
| Area% [%] | 63.011 |  |  |  |  | Mw/Mn | 1.806 |
| [eta] | 10747.98573 |  |  |  |  | Mz+1/Mw | 2.367 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 359 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.877 | 39.031 | 1,779 |  |  | Mw | 675 |
| Peak top | 12.235 | 54.257 | 576 |  |  | Mz | 978 |
| Peak end | 12.955 | 1.771 | 25 |  |  | Mz+1 | 1,191 |
|  |  |  |  |  |  | Mv | 675 |
| Height [mV] | 52.874 |  |  |  |  | Mp | 670 |
| Area [mV*s] | 1972.794 |  |  |  |  | Mz/Mw | 1.448 |
| Area% [%] | 36.989 |  |  |  |  | Mw/Mn | 1.880 |
| [eta] | 675.37087 |  |  |  |  | Mz+1/Mw | 1.764 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 881 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.748 | 0.044 | 84,214 |  |  | Mw | 7,022 |
| Peak top | 12.235 | 54.257 | 576 |  |  | Mz | 17,215 |
| Peak end | 12.955 | 1.771 | 25 |  |  | Mz+1 | 25,390 |
|  |  |  |  |  |  | Mv | 7,022 |
| Height [mV] | 100.936 |  |  |  |  | Mp | 9,927 |
| Area [mV*s] | 5333.470 |  |  |  |  | Mz/Mw | 2.452 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 7.973 |
| [eta] | 7022.23219 |  |  |  |  | Mz+1/Mw | 3.616 |