Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/08 19:35:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_8wks_A_3 |  |  |  |  |  |  | Calculation date and time | 2023/11/09 10:06:03 |
| Database name | SMF run-2023-11-08.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2420 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 14 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 6,770 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.643 | 0.077 | 98,551 |  |  | Mw | 12,375 |
| Peak top | 11.158 | 47.512 | 9,353 |  |  | Mz | 20,527 |
| Peak end | 11.847 | 35.023 | 1,935 |  |  | Mz+1 | 29,385 |
|  |  |  |  |  |  | Mv | 12,375 |
| Height [mV] | 46.806 |  |  |  |  | Mp | 11,844 |
| Area [mV*s] | 3388.608 |  |  |  |  | Mz/Mw | 1.659 |
| Area% [%] | 63.685 |  |  |  |  | Mw/Mn | 1.828 |
| [eta] | 12374.90623 |  |  |  |  | Mz+1/Mw | 2.375 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 373 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.847 | 35.023 | 1,935 |  |  | Mw | 709 |
| Peak top | 12.238 | 52.516 | 570 |  |  | Mz | 1,043 |
| Peak end | 12.940 | 1.445 | 27 |  |  | Mz+1 | 1,283 |
|  |  |  |  |  |  | Mv | 709 |
| Height [mV] | 51.362 |  |  |  |  | Mp | 659 |
| Area [mV*s] | 1932.257 |  |  |  |  | Mz/Mw | 1.471 |
| Area% [%] | 36.315 |  |  |  |  | Mw/Mn | 1.903 |
| [eta] | 709.32108 |  |  |  |  | Mz+1/Mw | 1.809 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 936 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.643 | 0.077 | 98,551 |  |  | Mw | 8,139 |
| Peak top | 12.238 | 52.516 | 570 |  |  | Mz | 19,910 |
| Peak end | 12.940 | 1.445 | 27 |  |  | Mz+1 | 29,339 |
|  |  |  |  |  |  | Mv | 8,139 |
| Height [mV] | 98.168 |  |  |  |  | Mp | 11,844 |
| Area [mV*s] | 5320.865 |  |  |  |  | Mz/Mw | 2.446 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 8.697 |
| [eta] | 8138.58147 |  |  |  |  | Mz+1/Mw | 3.605 |