Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/08 21:55:52 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_8wks_A_3 |  |  |  |  |  |  | Calculation date and time | 2023/11/09 10:07:54 |
| Database name | SMF run-2023-11-08.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2427 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 21 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 6,644 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.553 | 0.172 | 113,020 |  |  | Mw | 11,853 |
| Peak top | 11.315 | 41.551 | 6,869 |  |  | Mz | 20,512 |
| Peak end | 11.802 | 37.765 | 2,188 |  |  | Mz+1 | 30,942 |
|  |  |  |  |  |  | Mv | 11,853 |
| Height [mV] | 40.469 |  |  |  |  | Mp | 9,592 |
| Area [mV*s] | 2810.097 |  |  |  |  | Mz/Mw | 1.730 |
| Area% [%] | 54.788 |  |  |  |  | Mw/Mn | 1.784 |
| [eta] | 11853.34248 |  |  |  |  | Mz+1/Mw | 2.610 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 387 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.802 | 37.765 | 2,188 |  |  | Mw | 762 |
| Peak top | 12.245 | 61.887 | 556 |  |  | Mz | 1,151 |
| Peak end | 12.925 | 1.914 | 29 |  |  | Mz+1 | 1,437 |
|  |  |  |  |  |  | Mv | 762 |
| Height [mV] | 60.324 |  |  |  |  | Mp | 644 |
| Area [mV*s] | 2318.982 |  |  |  |  | Mz/Mw | 1.511 |
| Area% [%] | 45.212 |  |  |  |  | Mw/Mn | 1.966 |
| [eta] | 761.58084 |  |  |  |  | Mz+1/Mw | 1.887 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 800 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.553 | 0.172 | 113,020 |  |  | Mw | 6,838 |
| Peak top | 12.245 | 61.887 | 556 |  |  | Mz | 19,537 |
| Peak end | 12.925 | 1.914 | 29 |  |  | Mz+1 | 30,855 |
|  |  |  |  |  |  | Mv | 6,838 |
| Height [mV] | 100.793 |  |  |  |  | Mp | 9,592 |
| Area [mV*s] | 5129.079 |  |  |  |  | Mz/Mw | 2.857 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 8.544 |
| [eta] | 6838.48612 |  |  |  |  | Mz+1/Mw | 4.512 |