Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/08 22:15:52 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_8wks_A_2 |  |  |  |  |  |  | Calculation date and time | 2023/11/09 10:08:07 |
| Database name | SMF run-2023-11-08.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2428 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 22 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 7,193 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.598 | 0.066 | 105,509 |  |  | Mw | 12,727 |
| Peak top | 11.275 | 41.427 | 7,449 |  |  | Mz | 21,826 |
| Peak end | 11.772 | 36.727 | 2,370 |  |  | Mz+1 | 32,609 |
|  |  |  |  |  |  | Mv | 12,727 |
| Height [mV] | 40.808 |  |  |  |  | Mp | 10,208 |
| Area [mV*s] | 2864.435 |  |  |  |  | Mz/Mw | 1.715 |
| Area% [%] | 54.552 |  |  |  |  | Mw/Mn | 1.769 |
| [eta] | 12726.96119 |  |  |  |  | Mz+1/Mw | 2.562 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 396 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.772 | 36.727 | 2,370 |  |  | Mw | 801 |
| Peak top | 12.242 | 61.838 | 563 |  |  | Mz | 1,235 |
| Peak end | 12.955 | 1.174 | 25 |  |  | Mz+1 | 1,555 |
|  |  |  |  |  |  | Mv | 801 |
| Height [mV] | 60.899 |  |  |  |  | Mp | 640 |
| Area [mV*s] | 2386.390 |  |  |  |  | Mz/Mw | 1.542 |
| Area% [%] | 45.448 |  |  |  |  | Mw/Mn | 2.021 |
| [eta] | 801.15633 |  |  |  |  | Mz+1/Mw | 1.941 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 818 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.598 | 0.066 | 105,509 |  |  | Mw | 7,307 |
| Peak top | 12.242 | 61.838 | 563 |  |  | Mz | 20,800 |
| Peak end | 12.955 | 1.174 | 25 |  |  | Mz+1 | 32,518 |
|  |  |  |  |  |  | Mv | 7,307 |
| Height [mV] | 101.707 |  |  |  |  | Mp | 10,208 |
| Area [mV*s] | 5250.825 |  |  |  |  | Mz/Mw | 2.847 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 8.931 |
| [eta] | 7306.93217 |  |  |  |  | Mz+1/Mw | 4.450 |