Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/08 22:35:52 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_8wks_A_1 |  |  |  |  |  |  | Calculation date and time | 2023/11/09 10:08:27 |
| Database name | SMF run-2023-11-08.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2429 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 23 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 7,136 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.613 | 0.168 | 103,130 |  |  | Mw | 11,988 |
| Peak top | 11.378 | 33.982 | 6,019 |  |  | Mz | 20,007 |
| Peak end | 11.742 | 32.753 | 2,564 |  |  | Mz+1 | 29,641 |
|  |  |  |  |  |  | Mv | 11,988 |
| Height [mV] | 32.734 |  |  |  |  | Mp | 9,622 |
| Area [mV*s] | 2141.699 |  |  |  |  | Mz/Mw | 1.669 |
| Area% [%] | 47.954 |  |  |  |  | Mw/Mn | 1.680 |
| [eta] | 11987.73301 |  |  |  |  | Mz+1/Mw | 2.473 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 398 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.742 | 32.753 | 2,564 |  |  | Mw | 824 |
| Peak top | 12.245 | 60.753 | 556 |  |  | Mz | 1,304 |
| Peak end | 12.955 | 2.212 | 25 |  |  | Mz+1 | 1,665 |
|  |  |  |  |  |  | Mv | 824 |
| Height [mV] | 58.975 |  |  |  |  | Mp | 629 |
| Area [mV*s] | 2324.492 |  |  |  |  | Mz/Mw | 1.582 |
| Area% [%] | 52.046 |  |  |  |  | Mw/Mn | 2.071 |
| [eta] | 823.91196 |  |  |  |  | Mz+1/Mw | 2.021 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 727 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.613 | 0.168 | 103,130 |  |  | Mw | 6,177 |
| Peak top | 12.245 | 60.753 | 556 |  |  | Mz | 18,708 |
| Peak end | 12.955 | 2.212 | 25 |  |  | Mz+1 | 29,505 |
|  |  |  |  |  |  | Mv | 6,177 |
| Height [mV] | 91.710 |  |  |  |  | Mp | 629 |
| Area [mV*s] | 4466.191 |  |  |  |  | Mz/Mw | 3.029 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 8.499 |
| [eta] | 6177.36531 |  |  |  |  | Mz+1/Mw | 4.776 |