Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/21 16:55:45 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | AL_EVA_8w_A_4 |  |  |  |  |  |  | Calculation date and time | 2023/11/22 12:39:53 |
| Database name | SMF run-2023-11-21.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2442 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 6 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 9,304 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.088 | 0.259 | 239,502 |  |  | Mw | 17,118 |
| Peak top | 11.082 | 34.539 | 10,788 |  |  | Mz | 30,906 |
| Peak end | 11.697 | 30.243 | 2,878 |  |  | Mz+1 | 52,139 |
|  |  |  |  |  |  | Mv | 17,118 |
| Height [mV] | 30.827 |  |  |  |  | Mp | 14,394 |
| Area [mV*s] | 2381.738 |  |  |  |  | Mz/Mw | 1.806 |
| Area% [%] | 47.375 |  |  |  |  | Mw/Mn | 1.840 |
| [eta] | 17117.66381 |  |  |  |  | Mz+1/Mw | 3.046 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 366 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.697 | 30.243 | 2,878 |  |  | Mw | 798 |
| Peak top | 12.262 | 73.228 | 525 |  |  | Mz | 1,349 |
| Peak end | 12.970 | 6.983 | 23 |  |  | Mz+1 | 1,798 |
|  |  |  |  |  |  | Mv | 798 |
| Height [mV] | 67.472 |  |  |  |  | Mp | 594 |
| Area [mV*s] | 2645.646 |  |  |  |  | Mz/Mw | 1.690 |
| Area% [%] | 52.625 |  |  |  |  | Mw/Mn | 2.182 |
| [eta] | 798.33265 |  |  |  |  | Mz+1/Mw | 2.253 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 672 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.088 | 0.259 | 239,502 |  |  | Mw | 8,530 |
| Peak top | 12.262 | 73.228 | 525 |  |  | Mz | 29,450 |
| Peak end | 12.970 | 6.983 | 23 |  |  | Mz+1 | 52,025 |
|  |  |  |  |  |  | Mv | 8,530 |
| Height [mV] | 98.299 |  |  |  |  | Mp | 594 |
| Area [mV*s] | 5027.384 |  |  |  |  | Mz/Mw | 3.453 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 12.702 |
| [eta] | 8529.66421 |  |  |  |  | Mz+1/Mw | 6.099 |