Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/21 17:15:47 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | AL_POE_8w_A_4 |  |  |  |  |  |  | Calculation date and time | 2023/11/22 12:40:16 |
| Database name | SMF run-2023-11-21.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2443 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 7 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 10,029 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.163 | 0.167 | 211,009 |  |  | Mw | 18,521 |
| Peak top | 10.882 | 47.478 | 15,316 |  |  | Mz | 30,915 |
| Peak end | 11.712 | 34.072 | 2,771 |  |  | Mz+1 | 45,019 |
|  |  |  |  |  |  | Mv | 18,521 |
| Height [mV] | 45.474 |  |  |  |  | Mp | 18,068 |
| Area [mV*s] | 3605.162 |  |  |  |  | Mz/Mw | 1.669 |
| Area% [%] | 57.279 |  |  |  |  | Mw/Mn | 1.847 |
| [eta] | 18520.78289 |  |  |  |  | Mz+1/Mw | 2.431 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 406 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.712 | 34.072 | 2,771 |  |  | Mw | 843 |
| Peak top | 12.238 | 72.710 | 570 |  |  | Mz | 1,359 |
| Peak end | 12.970 | 4.237 | 23 |  |  | Mz+1 | 1,765 |
|  |  |  |  |  |  | Mv | 843 |
| Height [mV] | 69.255 |  |  |  |  | Mp | 644 |
| Area [mV*s] | 2688.880 |  |  |  |  | Mz/Mw | 1.612 |
| Area% [%] | 42.721 |  |  |  |  | Mw/Mn | 2.079 |
| [eta] | 843.22596 |  |  |  |  | Mz+1/Mw | 2.093 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 901 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.163 | 0.167 | 211,009 |  |  | Mw | 10,969 |
| Peak top | 12.238 | 72.710 | 570 |  |  | Mz | 29,944 |
| Peak end | 12.970 | 4.237 | 23 |  |  | Mz+1 | 44,955 |
|  |  |  |  |  |  | Mv | 10,969 |
| Height [mV] | 114.729 |  |  |  |  | Mp | 18,068 |
| Area [mV*s] | 6294.041 |  |  |  |  | Mz/Mw | 2.730 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 12.178 |
| [eta] | 10968.74752 |  |  |  |  | Mz+1/Mw | 4.098 |