Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/12 17:15:47 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_4wks_A_4 |  |  |  |  |  |  | Calculation date and time | 2023/10/13 10:16:15 |
| Database name | SMF run-2023-10-12.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2372 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 7 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 13,237 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.908 | 1.834 | 327,645 |  |  | Mw | 35,056 |
| Peak top | 10.605 | 46.309 | 23,886 |  |  | Mz | 70,994 |
| Peak end | 11.907 | 11.979 | 1,634 |  |  | Mz+1 | 112,987 |
|  |  |  |  |  |  | Mv | 35,056 |
| Height [mV] | 44.052 |  |  |  |  | Mp | 27,470 |
| Area [mV*s] | 4218.703 |  |  |  |  | Mz/Mw | 2.025 |
| Area% [%] | 8.376 |  |  |  |  | Mw/Mn | 2.648 |
| [eta] | 35056.31932 |  |  |  |  | Mz+1/Mw | 3.223 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 346 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.907 | 11.979 | 1,634 |  |  | Mw | 624 |
| Peak top | 12.210 | 12.887 | 629 |  |  | Mz | 919 |
| Peak end | 12.685 | 10.060 | 94 |  |  | Mz+1 | 1,119 |
|  |  |  |  |  |  | Mv | 624 |
| Height [mV] | 10.229 |  |  |  |  | Mp | 1,634 |
| Area [mV*s] | 419.815 |  |  |  |  | Mz/Mw | 1.473 |
| Area% [%] | 0.834 |  |  |  |  | Mw/Mn | 1.804 |
| [eta] | 623.60533 |  |  |  |  | Mz+1/Mw | 1.794 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.685 | 10.060 | 94 |  |  | Mw | 5 |
| Peak top | 13.042 | 1000.000 | 15 |  |  | Mz | 14 |
| Peak end | 14.768 | 3.296 | 1 |  |  | Mz+1 | 25 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 997.135 |  |  |  |  | Mp | 16 |
| Area [mV*s] | 45727.675 |  |  |  |  | Mz/Mw | 2.621 |
| Area% [%] | 90.790 |  |  |  |  | Mw/Mn | 2.887 |
| [eta] | 5.38325 |  |  |  |  | Mz+1/Mw | 4.662 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.908 | 1.834 | 327,645 |  |  | Mw | 2,946 |
| Peak top | 13.042 | 1000.000 | 15 |  |  | Mz | 70,753 |
| Peak end | 14.768 | 3.296 | 1 |  |  | Mz+1 | 112,985 |
|  |  |  |  |  |  | Mv | 2,946 |
| Height [mV] | 1051.416 |  |  |  |  | Mp | 16 |
| Area [mV*s] | 50366.193 |  |  |  |  | Mz/Mw | 24.013 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1434.540 |
| [eta] | 2946.42391 |  |  |  |  | Mz+1/Mw | 38.346 |