Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/12 17:35:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_4wks_A_3 |  |  |  |  |  |  | Calculation date and time | 2023/10/13 10:16:28 |
| Database name | SMF run-2023-10-12.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2373 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 8 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 10,855 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.073 | 1.201 | 245,714 |  |  | Mw | 27,381 |
| Peak top | 10.722 | 45.754 | 19,898 |  |  | Mz | 53,250 |
| Peak end | 11.922 | 14.422 | 1,564 |  |  | Mz+1 | 82,714 |
|  |  |  |  |  |  | Mv | 27,381 |
| Height [mV] | 44.037 |  |  |  |  | Mp | 23,280 |
| Area [mV*s] | 4059.832 |  |  |  |  | Mz/Mw | 1.945 |
| Area% [%] | 8.426 |  |  |  |  | Mw/Mn | 2.522 |
| [eta] | 27380.64453 |  |  |  |  | Mz+1/Mw | 3.021 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 315 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.922 | 14.422 | 1,564 |  |  | Mw | 611 |
| Peak top | 11.922 | 14.422 | 1,564 |  |  | Mz | 902 |
| Peak end | 12.745 | 8.996 | 71 |  |  | Mz+1 | 1,087 |
|  |  |  |  |  |  | Mv | 611 |
| Height [mV] | 12.330 |  |  |  |  | Mp | 1,565 |
| Area [mV*s] | 498.851 |  |  |  |  | Mz/Mw | 1.477 |
| Area% [%] | 1.035 |  |  |  |  | Mw/Mn | 1.937 |
| [eta] | 611.04756 |  |  |  |  | Mz+1/Mw | 1.779 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.745 | 8.996 | 71 |  |  | Mw | 5 |
| Peak top | 13.068 | 1000.000 | 13 |  |  | Mz | 12 |
| Peak end | 14.753 | 2.978 | 1 |  |  | Mz+1 | 20 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 997.549 |  |  |  |  | Mp | 13 |
| Area [mV*s] | 43623.829 |  |  |  |  | Mz/Mw | 2.476 |
| Area% [%] | 90.539 |  |  |  |  | Mw/Mn | 2.698 |
| [eta] | 4.98679 |  |  |  |  | Mz+1/Mw | 4.089 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.073 | 1.201 | 245,714 |  |  | Mw | 2,318 |
| Peak top | 13.068 | 1000.000 | 13 |  |  | Mz | 53,003 |
| Peak end | 14.753 | 2.978 | 1 |  |  | Mz+1 | 82,711 |
|  |  |  |  |  |  | Mv | 2,318 |
| Height [mV] | 1053.916 |  |  |  |  | Mp | 13 |
| Area [mV*s] | 48182.512 |  |  |  |  | Mz/Mw | 22.867 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1135.400 |
| [eta] | 2317.91930 |  |  |  |  | Mz+1/Mw | 35.683 |