Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/12 17:55:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_4wks_A_2 |  |  |  |  |  |  | Calculation date and time | 2023/10/13 10:16:39 |
| Database name | SMF run-2023-10-12.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2374 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 9 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 12,201 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.597 | 0.625 | 581,185 |  |  | Mw | 36,726 |
| Peak top | 10.612 | 45.138 | 23,642 |  |  | Mz | 85,459 |
| Peak end | 11.965 | 12.178 | 1,378 |  |  | Mz+1 | 160,526 |
|  |  |  |  |  |  | Mv | 36,726 |
| Height [mV] | 44.059 |  |  |  |  | Mp | 27,264 |
| Area [mV*s] | 4334.174 |  |  |  |  | Mz/Mw | 2.327 |
| Area% [%] | 8.633 |  |  |  |  | Mw/Mn | 3.010 |
| [eta] | 36726.02007 |  |  |  |  | Mz+1/Mw | 4.371 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 318 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.965 | 12.178 | 1,378 |  |  | Mw | 546 |
| Peak top | 12.217 | 13.454 | 614 |  |  | Mz | 783 |
| Peak end | 12.697 | 9.435 | 90 |  |  | Mz+1 | 945 |
|  |  |  |  |  |  | Mv | 546 |
| Height [mV] | 12.014 |  |  |  |  | Mp | 1,365 |
| Area [mV*s] | 461.387 |  |  |  |  | Mz/Mw | 1.434 |
| Area% [%] | 0.919 |  |  |  |  | Mw/Mn | 1.720 |
| [eta] | 546.27003 |  |  |  |  | Mz+1/Mw | 1.730 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.697 | 9.435 | 90 |  |  | Mw | 5 |
| Peak top | 13.050 | 1000.000 | 14 |  |  | Mz | 14 |
| Peak end | 15.105 | 2.090 | 1 |  |  | Mz+1 | 24 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 998.373 |  |  |  |  | Mp | 15 |
| Area [mV*s] | 45407.388 |  |  |  |  | Mz/Mw | 2.604 |
| Area% [%] | 90.448 |  |  |  |  | Mw/Mn | 2.835 |
| [eta] | 5.25175 |  |  |  |  | Mz+1/Mw | 4.611 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.597 | 0.625 | 581,185 |  |  | Mw | 3,180 |
| Peak top | 13.050 | 1000.000 | 14 |  |  | Mz | 85,198 |
| Peak end | 15.105 | 2.090 | 1 |  |  | Mz+1 | 160,524 |
|  |  |  |  |  |  | Mv | 3,180 |
| Height [mV] | 1054.446 |  |  |  |  | Mp | 15 |
| Area [mV*s] | 50202.949 |  |  |  |  | Mz/Mw | 26.788 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1553.083 |
| [eta] | 3180.43988 |  |  |  |  | Mz+1/Mw | 50.472 |