Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/12 18:15:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_4wks_A_1 |  |  |  |  |  |  | Calculation date and time | 2023/10/13 10:17:00 |
| Database name | SMF run-2023-10-12.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2375 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 10 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 19,590 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.653 | 0.792 | 522,257 |  |  | Mw | 43,643 |
| Peak top | 10.515 | 27.672 | 27,401 |  |  | Mz | 89,186 |
| Peak end | 11.892 | 6.760 | 1,705 |  |  | Mz+1 | 153,376 |
|  |  |  |  |  |  | Mv | 43,643 |
| Height [mV] | 23.449 |  |  |  |  | Mp | 30,133 |
| Area [mV*s] | 2081.127 |  |  |  |  | Mz/Mw | 2.044 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.228 |
| [eta] | 43642.88881 |  |  |  |  | Mz+1/Mw | 3.514 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 19,590 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.653 | 0.792 | 522,257 |  |  | Mw | 43,643 |
| Peak top | 10.515 | 27.672 | 27,401 |  |  | Mz | 89,186 |
| Peak end | 11.892 | 6.760 | 1,705 |  |  | Mz+1 | 153,376 |
|  |  |  |  |  |  | Mv | 43,643 |
| Height [mV] | 23.449 |  |  |  |  | Mp | 30,133 |
| Area [mV*s] | 2081.127 |  |  |  |  | Mz/Mw | 2.044 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.228 |
| [eta] | 43642.88881 |  |  |  |  | Mz+1/Mw | 3.514 |