Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/24 16:15:36 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_4wks_A_1 |  |  |  |  |  |  | Calculation date and time | 2023/10/25 10:05:51 |
| Database name | SMF run-2023-10-24.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2385 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 4 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 15,415 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.758 | 1.447 | 429,720 |  |  | Mw | 37,085 |
| Peak top | 10.468 | 58.313 | 29,392 |  |  | Mz | 74,137 |
| Peak end | 11.742 | 22.662 | 2,564 |  |  | Mz+1 | 125,516 |
|  |  |  |  |  |  | Mv | 37,085 |
| Height [mV] | 56.363 |  |  |  |  | Mp | 31,665 |
| Area [mV*s] | 5063.871 |  |  |  |  | Mz/Mw | 1.999 |
| Area% [%] | 9.672 |  |  |  |  | Mw/Mn | 2.406 |
| [eta] | 37085.47768 |  |  |  |  | Mz+1/Mw | 3.385 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 334 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.742 | 22.662 | 2,564 |  |  | Mw | 714 |
| Peak top | 12.272 | 50.911 | 506 |  |  | Mz | 1,217 |
| Peak end | 12.730 | 28.205 | 77 |  |  | Mz+1 | 1,610 |
|  |  |  |  |  |  | Mv | 714 |
| Height [mV] | 48.430 |  |  |  |  | Mp | 587 |
| Area [mV*s] | 2051.875 |  |  |  |  | Mz/Mw | 1.705 |
| Area% [%] | 3.919 |  |  |  |  | Mw/Mn | 2.137 |
| [eta] | 713.65651 |  |  |  |  | Mz+1/Mw | 2.256 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.730 | 28.205 | 77 |  |  | Mw | 5 |
| Peak top | 13.048 | 1000.000 | 15 |  |  | Mz | 15 |
| Peak end | 14.858 | 3.242 | 1 |  |  | Mz+1 | 27 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 997.291 |  |  |  |  | Mp | 15 |
| Area [mV*s] | 45241.731 |  |  |  |  | Mz/Mw | 2.729 |
| Area% [%] | 86.409 |  |  |  |  | Mw/Mn | 2.925 |
| [eta] | 5.49136 |  |  |  |  | Mz+1/Mw | 4.946 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.758 | 1.447 | 429,720 |  |  | Mw | 3,620 |
| Peak top | 13.048 | 1000.000 | 15 |  |  | Mz | 73,476 |
| Peak end | 14.858 | 3.242 | 1 |  |  | Mz+1 | 125,500 |
|  |  |  |  |  |  | Mv | 3,620 |
| Height [mV] | 1102.084 |  |  |  |  | Mp | 15 |
| Area [mV*s] | 52357.477 |  |  |  |  | Mz/Mw | 20.300 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1666.345 |
| [eta] | 3619.51833 |  |  |  |  | Mz+1/Mw | 34.673 |