Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/24 16:35:42 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_4wks_A_2 |  |  |  |  |  |  | Calculation date and time | 2023/10/25 10:06:11 |
| Database name | SMF run-2023-10-24.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2386 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 5 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 14,355 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.623 | 0.437 | 552,592 |  |  | Mw | 35,149 |
| Peak top | 10.547 | 66.676 | 26,117 |  |  | Mz | 75,798 |
| Peak end | 11.742 | 27.995 | 2,564 |  |  | Mz+1 | 140,641 |
|  |  |  |  |  |  | Mv | 35,149 |
| Height [mV] | 65.726 |  |  |  |  | Mp | 28,811 |
| Area [mV*s] | 6018.992 |  |  |  |  | Mz/Mw | 2.156 |
| Area% [%] | 11.712 |  |  |  |  | Mw/Mn | 2.449 |
| [eta] | 35149.01967 |  |  |  |  | Mz+1/Mw | 4.001 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 328 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.742 | 27.995 | 2,564 |  |  | Mw | 737 |
| Peak top | 12.258 | 55.345 | 531 |  |  | Mz | 1,258 |
| Peak end | 12.760 | 25.176 | 66 |  |  | Mz+1 | 1,645 |
|  |  |  |  |  |  | Mv | 737 |
| Height [mV] | 53.938 |  |  |  |  | Mp | 615 |
| Area [mV*s] | 2364.036 |  |  |  |  | Mz/Mw | 1.707 |
| Area% [%] | 4.600 |  |  |  |  | Mw/Mn | 2.250 |
| [eta] | 737.32585 |  |  |  |  | Mz+1/Mw | 2.231 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.760 | 25.176 | 66 |  |  | Mw | 5 |
| Peak top | 13.075 | 1000.000 | 12 |  |  | Mz | 13 |
| Peak end | 14.933 | 2.120 | 1 |  |  | Mz+1 | 23 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 998.376 |  |  |  |  | Mp | 13 |
| Area [mV*s] | 43008.817 |  |  |  |  | Mz/Mw | 2.607 |
| Area% [%] | 83.688 |  |  |  |  | Mw/Mn | 2.720 |
| [eta] | 5.05300 |  |  |  |  | Mz+1/Mw | 4.631 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.623 | 0.437 | 552,592 |  |  | Mw | 4,155 |
| Peak top | 13.075 | 1000.000 | 12 |  |  | Mz | 75,112 |
| Peak end | 14.933 | 2.120 | 1 |  |  | Mz+1 | 140,622 |
|  |  |  |  |  |  | Mv | 4,155 |
| Height [mV] | 1118.040 |  |  |  |  | Mp | 13 |
| Area [mV*s] | 51391.845 |  |  |  |  | Mz/Mw | 18.078 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1872.418 |
| [eta] | 4154.78490 |  |  |  |  | Mz+1/Mw | 33.846 |