Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/24 16:55:45 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_4wks_A_3 |  |  |  |  |  |  | Calculation date and time | 2023/10/25 10:06:31 |
| Database name | SMF run-2023-10-24.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2387 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 6 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 14,498 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.893 | 0.571 | 336,516 |  |  | Mw | 31,780 |
| Peak top | 10.548 | 57.239 | 26,051 |  |  | Mz | 59,138 |
| Peak end | 11.727 | 22.285 | 2,666 |  |  | Mz+1 | 95,359 |
|  |  |  |  |  |  | Mv | 31,780 |
| Height [mV] | 56.283 |  |  |  |  | Mp | 28,667 |
| Area [mV*s] | 4793.701 |  |  |  |  | Mz/Mw | 1.861 |
| Area% [%] | 9.712 |  |  |  |  | Mw/Mn | 2.192 |
| [eta] | 31779.60488 |  |  |  |  | Mz+1/Mw | 3.001 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 309 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.727 | 22.285 | 2,666 |  |  | Mw | 713 |
| Peak top | 12.275 | 52.112 | 500 |  |  | Mz | 1,256 |
| Peak end | 12.775 | 23.799 | 62 |  |  | Mz+1 | 1,676 |
|  |  |  |  |  |  | Mv | 713 |
| Height [mV] | 50.754 |  |  |  |  | Mp | 584 |
| Area [mV*s] | 2203.940 |  |  |  |  | Mz/Mw | 1.761 |
| Area% [%] | 4.465 |  |  |  |  | Mw/Mn | 2.310 |
| [eta] | 713.43713 |  |  |  |  | Mz+1/Mw | 2.349 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.775 | 23.799 | 62 |  |  | Mw | 5 |
| Peak top | 13.087 | 1000.000 | 12 |  |  | Mz | 12 |
| Peak end | 14.978 | 1.987 | 1 |  |  | Mz+1 | 22 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 998.453 |  |  |  |  | Mp | 12 |
| Area [mV*s] | 42359.829 |  |  |  |  | Mz/Mw | 2.558 |
| Area% [%] | 85.823 |  |  |  |  | Mw/Mn | 2.636 |
| [eta] | 4.84190 |  |  |  |  | Mz+1/Mw | 4.486 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.893 | 0.571 | 336,516 |  |  | Mw | 3,123 |
| Peak top | 13.087 | 1000.000 | 12 |  |  | Mz | 58,469 |
| Peak end | 14.978 | 1.987 | 1 |  |  | Mz+1 | 95,338 |
|  |  |  |  |  |  | Mv | 3,123 |
| Height [mV] | 1105.490 |  |  |  |  | Mp | 12 |
| Area [mV*s] | 49357.469 |  |  |  |  | Mz/Mw | 18.725 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1459.422 |
| [eta] | 3122.51389 |  |  |  |  | Mz+1/Mw | 30.532 |