Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/09/26 15:35:36 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_2wks_A_1 |  |  |  |  |  |  | Calculation date and time | 2023/09/27 14:45:11 |
| Database name | SMF run-2023-09-26.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2358 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 2 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 15,954 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.073 | 1.643 | 245,714 |  |  | Mw | 38,382 |
| Peak top | 10.512 | 7.638 | 27,539 |  |  | Mz | 69,168 |
| Peak end | 12.057 | 3.163 | 1,041 |  |  | Mz+1 | 100,430 |
|  |  |  |  |  |  | Mv | 38,382 |
| Height [mV] | 5.262 |  |  |  |  | Mp | 32,297 |
| Area [mV*s] | 478.398 |  |  |  |  | Mz/Mw | 1.802 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.406 |
| [eta] | 38381.87979 |  |  |  |  | Mz+1/Mw | 2.617 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 15,954 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.073 | 1.643 | 245,714 |  |  | Mw | 38,382 |
| Peak top | 10.512 | 7.638 | 27,539 |  |  | Mz | 69,168 |
| Peak end | 12.057 | 3.163 | 1,041 |  |  | Mz+1 | 100,430 |
|  |  |  |  |  |  | Mv | 38,382 |
| Height [mV] | 5.262 |  |  |  |  | Mp | 32,297 |
| Area [mV*s] | 478.398 |  |  |  |  | Mz/Mw | 1.802 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.406 |
| [eta] | 38381.87979 |  |  |  |  | Mz+1/Mw | 2.617 |