Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/09/26 15:55:36 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_2wks_A_2 |  |  |  |  |  |  | Calculation date and time | 2023/09/27 14:45:33 |
| Database name | SMF run-2023-09-26.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2359 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 3 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 18,788 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.313 | 1.411 | 164,886 |  |  | Mw | 33,862 |
| Peak top | 10.510 | 9.031 | 27,608 |  |  | Mz | 52,407 |
| Peak end | 11.877 | 2.553 | 1,779 |  |  | Mz+1 | 70,853 |
|  |  |  |  |  |  | Mv | 33,862 |
| Height [mV] | 7.087 |  |  |  |  | Mp | 30,359 |
| Area [mV*s] | 543.672 |  |  |  |  | Mz/Mw | 1.548 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1.802 |
| [eta] | 33862.10711 |  |  |  |  | Mz+1/Mw | 2.092 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 18,788 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.313 | 1.411 | 164,886 |  |  | Mw | 33,862 |
| Peak top | 10.510 | 9.031 | 27,608 |  |  | Mz | 52,407 |
| Peak end | 11.877 | 2.553 | 1,779 |  |  | Mz+1 | 70,853 |
|  |  |  |  |  |  | Mv | 33,862 |
| Height [mV] | 7.087 |  |  |  |  | Mp | 30,359 |
| Area [mV*s] | 543.672 |  |  |  |  | Mz/Mw | 1.548 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1.802 |
| [eta] | 33862.10711 |  |  |  |  | Mz+1/Mw | 2.092 |