Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/09/26 16:15:36 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_2wks_A_3 |  |  |  |  |  |  | Calculation date and time | 2023/09/27 14:45:42 |
| Database name | SMF run-2023-09-26.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2360 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 4 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 13,831 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.508 | 0.858 | 121,139 |  |  | Mw | 27,127 |
| Peak top | 10.578 | 6.198 | 24,885 |  |  | Mz | 41,188 |
| Peak end | 12.012 | 2.242 | 1,197 |  |  | Mz+1 | 53,991 |
|  |  |  |  |  |  | Mv | 27,127 |
| Height [mV] | 4.748 |  |  |  |  | Mp | 26,250 |
| Area [mV*s] | 353.938 |  |  |  |  | Mz/Mw | 1.518 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1.961 |
| [eta] | 27126.68185 |  |  |  |  | Mz+1/Mw | 1.990 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 13,831 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.508 | 0.858 | 121,139 |  |  | Mw | 27,127 |
| Peak top | 10.578 | 6.198 | 24,885 |  |  | Mz | 41,188 |
| Peak end | 12.012 | 2.242 | 1,197 |  |  | Mz+1 | 53,991 |
|  |  |  |  |  |  | Mv | 27,127 |
| Height [mV] | 4.748 |  |  |  |  | Mp | 26,250 |
| Area [mV*s] | 353.938 |  |  |  |  | Mz/Mw | 1.518 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1.961 |
| [eta] | 27126.68185 |  |  |  |  | Mz+1/Mw | 1.990 |