Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/09/26 16:35:41 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_2wks_A_1 |  |  |  |  |  |  | Calculation date and time | 2023/09/27 14:45:50 |
| Database name | SMF run-2023-09-26.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2361 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 5 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 13,466 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.148 | 0.531 | 216,383 |  |  | Mw | 30,215 |
| Peak top | 10.593 | 18.574 | 24,319 |  |  | Mz | 52,188 |
| Peak end | 12.117 | 3.520 | 859 |  |  | Mz+1 | 76,463 |
|  |  |  |  |  |  | Mv | 30,215 |
| Height [mV] | 16.588 |  |  |  |  | Mp | 27,127 |
| Area [mV*s] | 1366.628 |  |  |  |  | Mz/Mw | 1.727 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.244 |
| [eta] | 30214.56741 |  |  |  |  | Mz+1/Mw | 2.531 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 13,466 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.148 | 0.531 | 216,383 |  |  | Mw | 30,215 |
| Peak top | 10.593 | 18.574 | 24,319 |  |  | Mz | 52,188 |
| Peak end | 12.117 | 3.520 | 859 |  |  | Mz+1 | 76,463 |
|  |  |  |  |  |  | Mv | 30,215 |
| Height [mV] | 16.588 |  |  |  |  | Mp | 27,127 |
| Area [mV*s] | 1366.628 |  |  |  |  | Mz/Mw | 1.727 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.244 |
| [eta] | 30214.56741 |  |  |  |  | Mz+1/Mw | 2.531 |