Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/09/26 16:55:45 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_2wks_A_2 |  |  |  |  |  |  | Calculation date and time | 2023/09/27 14:45:59 |
| Database name | SMF run-2023-09-26.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2362 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 6 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 10,398 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.298 | 1.536 | 168,938 |  |  | Mw | 27,571 |
| Peak top | 10.602 | 21.649 | 24,009 |  |  | Mz | 47,415 |
| Peak end | 12.327 | 4.029 | 414 |  |  | Mz+1 | 66,852 |
|  |  |  |  |  |  | Mv | 27,571 |
| Height [mV] | 19.040 |  |  |  |  | Mp | 26,450 |
| Area [mV*s] | 1618.081 |  |  |  |  | Mz/Mw | 1.720 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.651 |
| [eta] | 27570.93415 |  |  |  |  | Mz+1/Mw | 2.425 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 10,398 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.298 | 1.536 | 168,938 |  |  | Mw | 27,571 |
| Peak top | 10.602 | 21.649 | 24,009 |  |  | Mz | 47,415 |
| Peak end | 12.327 | 4.029 | 414 |  |  | Mz+1 | 66,852 |
|  |  |  |  |  |  | Mv | 27,571 |
| Height [mV] | 19.040 |  |  |  |  | Mp | 26,450 |
| Area [mV*s] | 1618.081 |  |  |  |  | Mz/Mw | 1.720 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.651 |
| [eta] | 27570.93415 |  |  |  |  | Mz+1/Mw | 2.425 |