Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/09/26 17:15:47 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_2wks_A_3 |  |  |  |  |  |  | Calculation date and time | 2023/09/27 14:46:10 |
| Database name | SMF run-2023-09-26.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2363 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 7 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 14,495 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.773 | 1.123 | 418,055 |  |  | Mw | 47,019 |
| Peak top | 10.383 | 27.036 | 33,348 |  |  | Mz | 94,300 |
| Peak end | 12.357 | 2.761 | 371 |  |  | Mz+1 | 147,794 |
|  |  |  |  |  |  | Mv | 47,019 |
| Height [mV] | 25.177 |  |  |  |  | Mp | 36,247 |
| Area [mV*s] | 2523.240 |  |  |  |  | Mz/Mw | 2.006 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 3.244 |
| [eta] | 47018.85133 |  |  |  |  | Mz+1/Mw | 3.143 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 14,495 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.773 | 1.123 | 418,055 |  |  | Mw | 47,019 |
| Peak top | 10.383 | 27.036 | 33,348 |  |  | Mz | 94,300 |
| Peak end | 12.357 | 2.761 | 371 |  |  | Mz+1 | 147,794 |
|  |  |  |  |  |  | Mv | 47,019 |
| Height [mV] | 25.177 |  |  |  |  | Mp | 36,247 |
| Area [mV*s] | 2523.240 |  |  |  |  | Mz/Mw | 2.006 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 3.244 |
| [eta] | 47018.85133 |  |  |  |  | Mz+1/Mw | 3.143 |