Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/12 16:35:41 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | POE_2wks_A_4 |  |  |  |  |  |  | Calculation date and time | 2023/10/13 10:15:11 |
| Database name | SMF run-2023-10-12.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2370 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 5 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 12,323 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.072 | 1.002 | 246,416 |  |  | Mw | 25,240 |
| Peak top | 10.652 | 58.545 | 22,219 |  |  | Mz | 43,776 |
| Peak end | 11.763 | 23.866 | 2,423 |  |  | Mz+1 | 66,819 |
|  |  |  |  |  |  | Mv | 25,240 |
| Height [mV] | 57.287 |  |  |  |  | Mp | 24,507 |
| Area [mV*s] | 4621.115 |  |  |  |  | Mz/Mw | 1.734 |
| Area% [%] | 9.345 |  |  |  |  | Mw/Mn | 2.048 |
| [eta] | 25239.53886 |  |  |  |  | Mz+1/Mw | 2.647 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 314 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.763 | 23.866 | 2,423 |  |  | Mw | 699 |
| Peak top | 12.265 | 48.800 | 518 |  |  | Mz | 1,181 |
| Peak end | 12.772 | 21.543 | 63 |  |  | Mz+1 | 1,542 |
|  |  |  |  |  |  | Mv | 699 |
| Height [mV] | 47.280 |  |  |  |  | Mp | 604 |
| Area [mV*s] | 2033.200 |  |  |  |  | Mz/Mw | 1.690 |
| Area% [%] | 4.111 |  |  |  |  | Mw/Mn | 2.225 |
| [eta] | 698.89918 |  |  |  |  | Mz+1/Mw | 2.207 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.772 | 21.543 | 63 |  |  | Mw | 5 |
| Peak top | 13.083 | 1000.000 | 12 |  |  | Mz | 12 |
| Peak end | 15.437 | 2.035 | 1 |  |  | Mz+1 | 22 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 998.347 |  |  |  |  | Mp | 12 |
| Area [mV*s] | 42798.048 |  |  |  |  | Mz/Mw | 2.554 |
| Area% [%] | 86.544 |  |  |  |  | Mw/Mn | 2.653 |
| [eta] | 4.86493 |  |  |  |  | Mz+1/Mw | 4.439 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.072 | 1.002 | 246,416 |  |  | Mw | 2,391 |
| Peak top | 13.083 | 1000.000 | 12 |  |  | Mz | 43,187 |
| Peak end | 15.437 | 2.035 | 1 |  |  | Mz+1 | 66,798 |
|  |  |  |  |  |  | Mv | 2,391 |
| Height [mV] | 1102.913 |  |  |  |  | Mp | 12 |
| Area [mV*s] | 49452.363 |  |  |  |  | Mz/Mw | 18.059 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1129.042 |
| [eta] | 2391.47367 |  |  |  |  | Mz+1/Mw | 27.932 |