Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/12 16:55:45 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EVA_2wks_A_4 |  |  |  |  |  |  | Calculation date and time | 2023/10/13 10:15:50 |
| Database name | SMF run-2023-10-12.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2371 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 6 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 13,826 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.683 | 1.341 | 493,746 |  |  | Mw | 37,909 |
| Peak top | 10.587 | 38.782 | 24,569 |  |  | Mz | 87,451 |
| Peak end | 11.727 | 23.138 | 2,666 |  |  | Mz+1 | 152,873 |
|  |  |  |  |  |  | Mv | 37,909 |
| Height [mV] | 36.780 |  |  |  |  | Mp | 27,401 |
| Area [mV*s] | 3851.270 |  |  |  |  | Mz/Mw | 2.307 |
| Area% [%] | 7.403 |  |  |  |  | Mw/Mn | 2.742 |
| [eta] | 37909.39417 |  |  |  |  | Mz+1/Mw | 4.033 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 325 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.727 | 23.138 | 2,666 |  |  | Mw | 735 |
| Peak top | 12.257 | 50.833 | 534 |  |  | Mz | 1,271 |
| Peak end | 12.760 | 25.470 | 66 |  |  | Mz+1 | 1,683 |
|  |  |  |  |  |  | Mv | 735 |
| Height [mV] | 48.250 |  |  |  |  | Mp | 608 |
| Area [mV*s] | 2069.110 |  |  |  |  | Mz/Mw | 1.730 |
| Area% [%] | 3.977 |  |  |  |  | Mw/Mn | 2.260 |
| [eta] | 734.67188 |  |  |  |  | Mz+1/Mw | 2.291 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.760 | 25.470 | 66 |  |  | Mw | 6 |
| Peak top | 13.037 | 1000.000 | 16 |  |  | Mz | 14 |
| Peak end | 14.813 | 3.471 | 1 |  |  | Mz+1 | 24 |
|  |  |  |  |  |  | Mv | 6 |
| Height [mV] | 997.146 |  |  |  |  | Mp | 16 |
| Area [mV*s] | 46102.108 |  |  |  |  | Mz/Mw | 2.593 |
| Area% [%] | 88.620 |  |  |  |  | Mw/Mn | 2.945 |
| [eta] | 5.52982 |  |  |  |  | Mz+1/Mw | 4.252 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.683 | 1.341 | 493,746 |  |  | Mw | 2,841 |
| Peak top | 13.037 | 1000.000 | 16 |  |  | Mz | 86,414 |
| Peak end | 14.813 | 3.471 | 1 |  |  | Mz+1 | 152,850 |
|  |  |  |  |  |  | Mv | 2,841 |
| Height [mV] | 1082.176 |  |  |  |  | Mp | 16 |
| Area [mV*s] | 52022.489 |  |  |  |  | Mz/Mw | 30.421 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1340.787 |
| [eta] | 2840.58607 |  |  |  |  | Mz+1/Mw | 53.809 |