Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/21 15:55:35 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | AL_POE_2w_A_4 |  |  |  |  |  |  | Calculation date and time | 2023/11/21 16:35:41 |
| Database name | SMF run-2023-11-21.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2439 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 3 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 12,190 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.998 | 0.167 | 279,663 |  |  | Mw | 22,877 |
| Peak top | 10.708 | 96.688 | 20,324 |  |  | Mz | 38,147 |
| Peak end | 11.682 | 58.071 | 2,990 |  |  | Mz+1 | 57,471 |
|  |  |  |  |  |  | Mv | 22,877 |
| Height [mV] | 89.909 |  |  |  |  | Mp | 22,510 |
| Area [mV*s] | 7152.983 |  |  |  |  | Mz/Mw | 1.668 |
| Area% [%] | 58.010 |  |  |  |  | Mw/Mn | 1.877 |
| [eta] | 22876.72491 |  |  |  |  | Mz+1/Mw | 2.512 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 347 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.682 | 58.071 | 2,990 |  |  | Mw | 804 |
| Peak top | 12.257 | 140.754 | 534 |  |  | Mz | 1,390 |
| Peak end | 13.000 | 15.640 | 19 |  |  | Mz+1 | 1,865 |
|  |  |  |  |  |  | Mv | 804 |
| Height [mV] | 127.988 |  |  |  |  | Mp | 608 |
| Area [mV*s] | 5177.696 |  |  |  |  | Mz/Mw | 1.729 |
| Area% [%] | 41.990 |  |  |  |  | Mw/Mn | 2.315 |
| [eta] | 804.01621 |  |  |  |  | Mz+1/Mw | 2.319 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 796 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.998 | 0.167 | 279,663 |  |  | Mw | 13,608 |
| Peak top | 12.257 | 140.754 | 534 |  |  | Mz | 37,235 |
| Peak end | 13.000 | 15.640 | 19 |  |  | Mz+1 | 57,420 |
|  |  |  |  |  |  | Mv | 13,608 |
| Height [mV] | 217.897 |  |  |  |  | Mp | 22,510 |
| Area [mV*s] | 12330.679 |  |  |  |  | Mz/Mw | 2.736 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 17.099 |
| [eta] | 13608.31544 |  |  |  |  | Mz+1/Mw | 4.219 |