Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/11/21 16:15:36 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | AL_EVA_2w_A_4 |  |  |  |  |  |  | Calculation date and time | 2023/11/21 16:35:58 |
| Database name | SMF run-2023-11-21.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2440 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 4 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 8,899 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.373 | 0.128 | 149,752 |  |  | Mw | 16,208 |
| Peak top | 11.202 | 61.931 | 8,608 |  |  | Mz | 28,362 |
| Peak end | 11.697 | 58.431 | 2,878 |  |  | Mz+1 | 42,508 |
|  |  |  |  |  |  | Mv | 16,208 |
| Height [mV] | 55.620 |  |  |  |  | Mp | 13,091 |
| Area [mV*s] | 4238.730 |  |  |  |  | Mz/Mw | 1.750 |
| Area% [%] | 46.712 |  |  |  |  | Mw/Mn | 1.821 |
| [eta] | 16207.89278 |  |  |  |  | Mz+1/Mw | 2.623 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 367 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.697 | 58.431 | 2,878 |  |  | Mw | 821 |
| Peak top | 12.253 | 129.031 | 540 |  |  | Mz | 1,383 |
| Peak end | 13.000 | 12.392 | 19 |  |  | Mz+1 | 1,824 |
|  |  |  |  |  |  | Mv | 821 |
| Height [mV] | 119.164 |  |  |  |  | Mp | 615 |
| Area [mV*s] | 4835.391 |  |  |  |  | Mz/Mw | 1.684 |
| Area% [%] | 53.288 |  |  |  |  | Mw/Mn | 2.236 |
| [eta] | 821.35041 |  |  |  |  | Mz+1/Mw | 2.220 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 665 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.373 | 0.128 | 149,752 |  |  | Mw | 8,009 |
| Peak top | 12.253 | 129.031 | 540 |  |  | Mz | 26,887 |
| Peak end | 13.000 | 12.392 | 19 |  |  | Mz+1 | 42,394 |
|  |  |  |  |  |  | Mv | 8,009 |
| Height [mV] | 174.784 |  |  |  |  | Mp | 615 |
| Area [mV*s] | 9074.121 |  |  |  |  | Mz/Mw | 3.357 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 12.038 |
| [eta] | 8008.75754 |  |  |  |  | Mz+1/Mw | 5.293 |