Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/07/21 17:35:48 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_EVA_unaged_1 |  |  |  |  |  |  | Calculation date and time | 2023/07/21 18:50:36 |
| Database name | SMF run-2023-07-21.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2293 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 8 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 16,172 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.173 | 0.353 | 1,328,036 |  |  | Mw | 42,863 |
| Peak top | 10.487 | 91.510 | 28,595 |  |  | Mz | 115,731 |
| Peak end | 11.877 | 11.617 | 1,779 |  |  | Mz+1 | 310,084 |
|  |  |  |  |  |  | Mv | 42,863 |
| Height [mV] | 92.044 |  |  |  |  | Mp | 31,122 |
| Area [mV*s] | 8367.151 |  |  |  |  | Mz/Mw | 2.700 |
| Area% [%] | 96.965 |  |  |  |  | Mw/Mn | 2.650 |
| [eta] | 42863.04924 |  |  |  |  | Mz+1/Mw | 7.234 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 860 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.877 | 11.617 | 1,779 |  |  | Mw | 1,031 |
| Peak top | 11.877 | 11.617 | 1,779 |  |  | Mz | 1,188 |
| Peak end | 12.402 | -1.269 | 312 |  |  | Mz+1 | 1,311 |
|  |  |  |  |  |  | Mv | 1,031 |
| Height [mV] | 12.685 |  |  |  |  | Mp | 1,780 |
| Area [mV*s] | 261.873 |  |  |  |  | Mz/Mw | 1.152 |
| Area% [%] | 3.035 |  |  |  |  | Mw/Mn | 1.198 |
| [eta] | 1031.05886 |  |  |  |  | Mz+1/Mw | 1.272 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 10,501 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.173 | 0.353 | 1,328,036 |  |  | Mw | 41,594 |
| Peak top | 10.487 | 91.510 | 28,595 |  |  | Mz | 115,645 |
| Peak end | 12.402 | -1.269 | 312 |  |  | Mz+1 | 310,082 |
|  |  |  |  |  |  | Mv | 41,594 |
| Height [mV] | 104.729 |  |  |  |  | Mp | 31,122 |
| Area [mV*s] | 8629.025 |  |  |  |  | Mz/Mw | 2.780 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 3.961 |
| [eta] | 41593.53309 |  |  |  |  | Mz+1/Mw | 7.455 |