Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/07/21 17:55:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_EVA_unaged_2 |  |  |  |  |  |  | Calculation date and time | 2023/07/21 18:52:37 |
| Database name | SMF run-2023-07-21.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2294 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 9 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 18,179 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.368 | 1.723 | 903,184 |  |  | Mw | 43,515 |
| Peak top | 10.523 | 215.253 | 27,058 |  |  | Mz | 109,584 |
| Peak end | 11.772 | 25.400 | 2,370 |  |  | Mz+1 | 248,822 |
|  |  |  |  |  |  | Mv | 43,515 |
| Height [mV] | 215.954 |  |  |  |  | Mp | 29,173 |
| Area [mV*s] | 19028.470 |  |  |  |  | Mz/Mw | 2.518 |
| Area% [%] | 48.963 |  |  |  |  | Mw/Mn | 2.394 |
| [eta] | 43514.65696 |  |  |  |  | Mz+1/Mw | 5.718 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 1,019 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.772 | 25.400 | 2,370 |  |  | Mw | 1,306 |
| Peak top | 11.772 | 25.400 | 2,370 |  |  | Mz | 1,564 |
| Peak end | 12.402 | -2.813 | 312 |  |  | Mz+1 | 1,752 |
|  |  |  |  |  |  | Mv | 1,306 |
| Height [mV] | 27.504 |  |  |  |  | Mp | 2,371 |
| Area [mV*s] | 601.429 |  |  |  |  | Mz/Mw | 1.197 |
| Area% [%] | 1.548 |  |  |  |  | Mw/Mn | 1.283 |
| [eta] | 1306.45382 |  |  |  |  | Mz+1/Mw | 1.341 |

Peak 3 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.880 | -25.270 | 37 |  |  | Mw | 4 |
| Peak top | 13.282 | 999.498 | 3 |  |  | Mz | 8 |
| Peak end | 13.690 | 300.048 | 1 |  |  | Mz+1 | 12 |
|  |  |  |  |  |  | Mv | 4 |
| Height [mV] | 863.448 |  |  |  |  | Mp | 4 |
| Area [mV*s] | 19233.310 |  |  |  |  | Mz/Mw | 1.805 |
| Area% [%] | 49.490 |  |  |  |  | Mw/Mn | 1.855 |
| [eta] | 4.33199 |  |  |  |  | Mz+1/Mw | 2.719 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 5 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.368 | 1.723 | 903,184 |  |  | Mw | 21,328 |
| Peak top | 13.282 | 999.498 | 3 |  |  | Mz | 109,470 |
| Peak end | 13.690 | 300.048 | 1 |  |  | Mz+1 | 248,818 |
|  |  |  |  |  |  | Mv | 21,328 |
| Height [mV] | 1106.906 |  |  |  |  | Mp | 29,173 |
| Area [mV*s] | 38863.210 |  |  |  |  | Mz/Mw | 5.133 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 4519.837 |
| [eta] | 21328.30539 |  |  |  |  | Mz+1/Mw | 11.666 |