Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/07/21 18:15:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_EVA_unaged_3 |  |  |  |  |  |  | Calculation date and time | 2023/07/21 18:53:02 |
| Database name | SMF run-2023-07-21.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2295 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 10 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 16,461 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.323 | 0.645 | 986,698 |  |  | Mw | 38,818 |
| Peak top | 10.578 | 217.985 | 24,885 |  |  | Mz | 94,627 |
| Peak end | 11.817 | 27.507 | 2,101 |  |  | Mz+1 | 223,079 |
|  |  |  |  |  |  | Mv | 38,818 |
| Height [mV] | 218.050 |  |  |  |  | Mp | 27,470 |
| Area [mV*s] | 19028.674 |  |  |  |  | Mz/Mw | 2.438 |
| Area% [%] | 39.774 |  |  |  |  | Mw/Mn | 2.358 |
| [eta] | 38818.41484 |  |  |  |  | Mz+1/Mw | 5.747 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 959 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.817 | 27.507 | 2,101 |  |  | Mw | 1,193 |
| Peak top | 11.817 | 27.507 | 2,101 |  |  | Mz | 1,402 |
| Peak end | 12.402 | -0.639 | 312 |  |  | Mz+1 | 1,558 |
|  |  |  |  |  |  | Mv | 1,193 |
| Height [mV] | 27.962 |  |  |  |  | Mp | 2,101 |
| Area [mV*s] | 573.063 |  |  |  |  | Mz/Mw | 1.175 |
| Area% [%] | 1.198 |  |  |  |  | Mw/Mn | 1.244 |
| [eta] | 1193.05994 |  |  |  |  | Mz+1/Mw | 1.306 |

Peak 3 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.910 | 12.393 | 31 |  |  | Mw | 5 |
| Peak top | 13.128 | 1000.000 | 9 |  |  | Mz | 9 |
| Peak end | 13.780 | 295.648 | 1 |  |  | Mz+1 | 13 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 916.522 |  |  |  |  | Mp | 10 |
| Area [mV*s] | 28240.622 |  |  |  |  | Mz/Mw | 1.918 |
| Area% [%] | 59.028 |  |  |  |  | Mw/Mn | 2.234 |
| [eta] | 4.83697 |  |  |  |  | Mz+1/Mw | 2.705 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 4 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.323 | 0.645 | 986,698 |  |  | Mw | 15,457 |
| Peak top | 13.128 | 1000.000 | 9 |  |  | Mz | 94,523 |
| Peak end | 13.780 | 295.648 | 1 |  |  | Mz+1 | 223,076 |
|  |  |  |  |  |  | Mv | 15,457 |
| Height [mV] | 1162.534 |  |  |  |  | Mp | 10 |
| Area [mV*s] | 47842.358 |  |  |  |  | Mz/Mw | 6.115 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 4215.031 |
| [eta] | 15456.66371 |  |  |  |  | Mz+1/Mw | 14.432 |