Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/02 15:55:36 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_EVA_unaged_4 |  |  |  |  |  |  | Calculation date and time | 2023/08/02 20:16:08 |
| Database name | SMF run-2023-08-02.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2300 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 3 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 12,850 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.638 | 1.262 | 537,190 |  |  | Mw | 32,596 |
| Peak top | 10.602 | 51.624 | 24,009 |  |  | Mz | 69,176 |
| Peak end | 11.937 | 8.481 | 1,498 |  |  | Mz+1 | 130,898 |
|  |  |  |  |  |  | Mv | 32,596 |
| Height [mV] | 51.538 |  |  |  |  | Mp | 26,517 |
| Area [mV*s] | 4535.099 |  |  |  |  | Mz/Mw | 2.122 |
| Area% [%] | 95.320 |  |  |  |  | Mw/Mn | 2.537 |
| [eta] | 32595.67064 |  |  |  |  | Mz+1/Mw | 4.016 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 645 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.937 | 8.481 | 1,498 |  |  | Mw | 809 |
| Peak top | 11.937 | 8.481 | 1,498 |  |  | Mz | 962 |
| Peak end | 12.505 | -1.054 | 207 |  |  | Mz+1 | 1,080 |
|  |  |  |  |  |  | Mv | 809 |
| Height [mV] | 9.195 |  |  |  |  | Mp | 1,498 |
| Area [mV*s] | 222.667 |  |  |  |  | Mz/Mw | 1.189 |
| Area% [%] | 4.680 |  |  |  |  | Mw/Mn | 1.256 |
| [eta] | 809.27340 |  |  |  |  | Mz+1/Mw | 1.335 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 6,813 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.638 | 1.262 | 537,190 |  |  | Mw | 31,108 |
| Peak top | 10.602 | 51.624 | 24,009 |  |  | Mz | 69,093 |
| Peak end | 12.505 | -1.054 | 207 |  |  | Mz+1 | 130,896 |
|  |  |  |  |  |  | Mv | 31,108 |
| Height [mV] | 60.733 |  |  |  |  | Mp | 26,517 |
| Area [mV*s] | 4757.767 |  |  |  |  | Mz/Mw | 2.221 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 4.566 |
| [eta] | 31108.04065 |  |  |  |  | Mz+1/Mw | 4.208 |