Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/02 16:15:36 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_EVA_unaged_5 |  |  |  |  |  |  | Calculation date and time | 2023/08/02 20:16:22 |
| Database name | SMF run-2023-08-02.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2301 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 4 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 14,788 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.073 | 1.147 | 245,714 |  |  | Mw | 34,229 |
| Peak top | 10.505 | 37.910 | 27,817 |  |  | Mz | 59,148 |
| Peak end | 12.237 | 2.467 | 573 |  |  | Mz+1 | 87,276 |
|  |  |  |  |  |  | Mv | 34,229 |
| Height [mV] | 36.166 |  |  |  |  | Mp | 29,319 |
| Area [mV*s] | 2979.122 |  |  |  |  | Mz/Mw | 1.728 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.315 |
| [eta] | 34228.86790 |  |  |  |  | Mz+1/Mw | 2.550 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 14,788 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.073 | 1.147 | 245,714 |  |  | Mw | 34,229 |
| Peak top | 10.505 | 37.910 | 27,817 |  |  | Mz | 59,148 |
| Peak end | 12.237 | 2.467 | 573 |  |  | Mz+1 | 87,276 |
|  |  |  |  |  |  | Mv | 34,229 |
| Height [mV] | 36.166 |  |  |  |  | Mp | 29,319 |
| Area [mV*s] | 2979.122 |  |  |  |  | Mz/Mw | 1.728 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.315 |
| [eta] | 34228.86790 |  |  |  |  | Mz+1/Mw | 2.550 |