Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/02 16:35:41 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_POE_unaged_1 |  |  |  |  |  |  | Calculation date and time | 2023/08/02 20:16:40 |
| Database name | SMF run-2023-08-02.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2302 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 5 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 20,476 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.073 | 1.387 | 245,714 |  |  | Mw | 38,064 |
| Peak top | 10.390 | 72.198 | 33,021 |  |  | Mz | 59,014 |
| Peak end | 12.147 | 3.336 | 779 |  |  | Mz+1 | 82,573 |
|  |  |  |  |  |  | Mv | 38,064 |
| Height [mV] | 69.976 |  |  |  |  | Mp | 34,094 |
| Area [mV*s] | 5116.020 |  |  |  |  | Mz/Mw | 1.550 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1.859 |
| [eta] | 38064.02341 |  |  |  |  | Mz+1/Mw | 2.169 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 20,476 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.073 | 1.387 | 245,714 |  |  | Mw | 38,064 |
| Peak top | 10.390 | 72.198 | 33,021 |  |  | Mz | 59,014 |
| Peak end | 12.147 | 3.336 | 779 |  |  | Mz+1 | 82,573 |
|  |  |  |  |  |  | Mv | 38,064 |
| Height [mV] | 69.976 |  |  |  |  | Mp | 34,094 |
| Area [mV*s] | 5116.020 |  |  |  |  | Mz/Mw | 1.550 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1.859 |
| [eta] | 38064.02341 |  |  |  |  | Mz+1/Mw | 2.169 |