Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/11 17:15:47 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_POE_unaged_2 |  |  |  |  |  |  | Calculation date and time | 2023/08/11 17:31:55 |
| Database name | SMF run-2023-08-11.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2311 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 7 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 15,746 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.343 | 0.726 | 157,111 |  |  | Mw | 28,234 |
| Peak top | 10.575 | 82.650 | 25,013 |  |  | Mz | 42,522 |
| Peak end | 12.042 | 5.506 | 1,091 |  |  | Mz+1 | 57,377 |
|  |  |  |  |  |  | Mv | 28,234 |
| Height [mV] | 79.742 |  |  |  |  | Mp | 26,990 |
| Area [mV*s] | 5650.240 |  |  |  |  | Mz/Mw | 1.506 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1.793 |
| [eta] | 28234.04524 |  |  |  |  | Mz+1/Mw | 2.032 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 15,746 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.343 | 0.726 | 157,111 |  |  | Mw | 28,234 |
| Peak top | 10.575 | 82.650 | 25,013 |  |  | Mz | 42,522 |
| Peak end | 12.042 | 5.506 | 1,091 |  |  | Mz+1 | 57,377 |
|  |  |  |  |  |  | Mv | 28,234 |
| Height [mV] | 79.742 |  |  |  |  | Mp | 26,990 |
| Area [mV*s] | 5650.240 |  |  |  |  | Mz/Mw | 1.506 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1.793 |
| [eta] | 28234.04524 |  |  |  |  | Mz+1/Mw | 2.032 |