Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/11 17:35:48 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_POE_unaged_3 |  |  |  |  |  |  | Calculation date and time | 2023/08/11 17:36:58 |
| Database name | SMF run-2023-08-11.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2312 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 8 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2,007 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.523 | 0.630 | 118,362 |  |  | Mw | 12,163 |
| Peak top | 11.125 | 53.824 | 9,958 |  |  | Mz | 25,601 |
| Peak end | 12.850 | 0.596 | 43 |  |  | Mz+1 | 37,966 |
|  |  |  |  |  |  | Mv | 12,163 |
| Height [mV] | 53.210 |  |  |  |  | Mp | 14,029 |
| Area [mV*s] | 5317.816 |  |  |  |  | Mz/Mw | 2.105 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 6.059 |
| [eta] | 12162.85574 |  |  |  |  | Mz+1/Mw | 3.122 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2,007 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.523 | 0.630 | 118,362 |  |  | Mw | 12,163 |
| Peak top | 11.125 | 53.824 | 9,958 |  |  | Mz | 25,601 |
| Peak end | 12.850 | 0.596 | 43 |  |  | Mz+1 | 37,966 |
|  |  |  |  |  |  | Mv | 12,163 |
| Height [mV] | 53.210 |  |  |  |  | Mp | 14,029 |
| Area [mV*s] | 5317.816 |  |  |  |  | Mz/Mw | 2.105 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 6.059 |
| [eta] | 12162.85574 |  |  |  |  | Mz+1/Mw | 3.122 |