Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/11 17:55:48 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_POE_unaged_4 |  |  |  |  |  |  | Calculation date and time | 2023/08/11 17:56:55 |
| Database name | SMF run-2023-08-11.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2313 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 9 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 15,920 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.313 | 2.290 | 164,886 |  |  | Mw | 30,078 |
| Peak top | 10.523 | 77.871 | 27,058 |  |  | Mz | 45,742 |
| Peak end | 12.132 | 5.327 | 818 |  |  | Mz+1 | 61,734 |
|  |  |  |  |  |  | Mv | 30,078 |
| Height [mV] | 74.277 |  |  |  |  | Mp | 28,524 |
| Area [mV*s] | 5387.384 |  |  |  |  | Mz/Mw | 1.521 |
| Area% [%] | 15.616 |  |  |  |  | Mw/Mn | 1.889 |
| [eta] | 30078.43119 |  |  |  |  | Mz+1/Mw | 2.052 |

Peak 2 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.790 | 8.191 | 57 |  |  | Mw | 5 |
| Peak top | 13.175 | 1000.000 | 7 |  |  | Mz | 9 |
| Peak end | 13.840 | 40.141 | 1 |  |  | Mz+1 | 15 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 980.094 |  |  |  |  | Mp | 7 |
| Area [mV*s] | 29111.776 |  |  |  |  | Mz/Mw | 2.046 |
| Area% [%] | 84.384 |  |  |  |  | Mw/Mn | 2.144 |
| [eta] | 4.60562 |  |  |  |  | Mz+1/Mw | 3.275 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 3 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.313 | 2.290 | 164,886 |  |  | Mw | 4,701 |
| Peak top | 13.175 | 1000.000 | 7 |  |  | Mz | 45,704 |
| Peak end | 13.840 | 40.141 | 1 |  |  | Mz+1 | 61,734 |
|  |  |  |  |  |  | Mv | 4,701 |
| Height [mV] | 1054.371 |  |  |  |  | Mp | 7 |
| Area [mV*s] | 34499.160 |  |  |  |  | Mz/Mw | 9.722 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1846.297 |
| [eta] | 4700.93004 |  |  |  |  | Mz+1/Mw | 13.132 |