Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/28 17:35:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_EVA_unaged_uncxx_1 |  |  |  |  |  |  | Calculation date and time | 2023/08/28 19:08:24 |
| Database name | SMF run-2023-08-28.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2323 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 8 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 9,901 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.953 | 0.464 | 302,579 |  |  | Mw | 29,421 |
| Peak top | 10.592 | 47.747 | 24,382 |  |  | Mz | 52,938 |
| Peak end | 12.550 | 3.494 | 171 |  |  | Mz+1 | 79,988 |
|  |  |  |  |  |  | Mv | 29,421 |
| Height [mV] | 45.903 |  |  |  |  | Mp | 26,854 |
| Area [mV*s] | 3992.260 |  |  |  |  | Mz/Mw | 1.799 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.971 |
| [eta] | 29420.52063 |  |  |  |  | Mz+1/Mw | 2.719 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 9,901 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.953 | 0.464 | 302,579 |  |  | Mw | 29,421 |
| Peak top | 10.592 | 47.747 | 24,382 |  |  | Mz | 52,938 |
| Peak end | 12.550 | 3.494 | 171 |  |  | Mz+1 | 79,988 |
|  |  |  |  |  |  | Mv | 29,421 |
| Height [mV] | 45.903 |  |  |  |  | Mp | 26,854 |
| Area [mV*s] | 3992.260 |  |  |  |  | Mz/Mw | 1.799 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 2.971 |
| [eta] | 29420.52063 |  |  |  |  | Mz+1/Mw | 2.719 |