Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/28 17:55:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_EVA_unaged_uncxx_2 |  |  |  |  |  |  | Calculation date and time | 2023/08/28 19:08:49 |
| Database name | SMF run-2023-08-28.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2324 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 9 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 639 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.208 | 0.586 | 195,779 |  |  | Mw | 6,542 |
| Peak top | 12.103 | 25.342 | 897 |  |  | Mz | 26,783 |
| Peak end | 12.925 | 7.198 | 29 |  |  | Mz+1 | 59,698 |
|  |  |  |  |  |  | Mv | 6,542 |
| Height [mV] | 19.606 |  |  |  |  | Mp | 2,218 |
| Area [mV*s] | 1837.448 |  |  |  |  | Mz/Mw | 4.094 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 10.240 |
| [eta] | 6542.03517 |  |  |  |  | Mz+1/Mw | 9.125 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 639 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.208 | 0.586 | 195,779 |  |  | Mw | 6,542 |
| Peak top | 12.103 | 25.342 | 897 |  |  | Mz | 26,783 |
| Peak end | 12.925 | 7.198 | 29 |  |  | Mz+1 | 59,698 |
|  |  |  |  |  |  | Mv | 6,542 |
| Height [mV] | 19.606 |  |  |  |  | Mp | 2,218 |
| Area [mV*s] | 1837.448 |  |  |  |  | Mz/Mw | 4.094 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 10.240 |
| [eta] | 6542.03517 |  |  |  |  | Mz+1/Mw | 9.125 |