Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/08/28 18:15:49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | DOW_EVA_unaged_uncxx_3 |  |  |  |  |  |  | Calculation date and time | 2023/08/28 19:09:09 |
| Database name | SMF run-2023-08-28.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2325 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 10 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 7,420 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.668 | 0.162 | 507,781 |  |  | Mw | 34,377 |
| Peak top | 10.510 | 66.066 | 27,608 |  |  | Mz | 70,156 |
| Peak end | 12.685 | 1.633 | 94 |  |  | Mz+1 | 118,598 |
|  |  |  |  |  |  | Mv | 34,377 |
| Height [mV] | 65.230 |  |  |  |  | Mp | 30,435 |
| Area [mV*s] | 6205.629 |  |  |  |  | Mz/Mw | 2.041 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 4.633 |
| [eta] | 34376.76747 |  |  |  |  | Mz+1/Mw | 3.450 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 7,420 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.668 | 0.162 | 507,781 |  |  | Mw | 34,377 |
| Peak top | 10.510 | 66.066 | 27,608 |  |  | Mz | 70,156 |
| Peak end | 12.685 | 1.633 | 94 |  |  | Mz+1 | 118,598 |
|  |  |  |  |  |  | Mv | 34,377 |
| Height [mV] | 65.230 |  |  |  |  | Mp | 30,435 |
| Area [mV*s] | 6205.629 |  |  |  |  | Mz/Mw | 2.041 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 4.633 |
| [eta] | 34376.76747 |  |  |  |  | Mz+1/Mw | 3.450 |