Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/24 17:15:48 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EPE_unaged_1 |  |  |  |  |  |  | Calculation date and time | 2023/10/25 10:06:39 |
| Database name | SMF run-2023-10-24.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2388 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 7 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 11,874 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.052 | 1.376 | 255,014 |  |  | Mw | 29,321 |
| Peak top | 10.673 | 35.248 | 21,478 |  |  | Mz | 58,174 |
| Peak end | 11.785 | 19.226 | 2,288 |  |  | Mz+1 | 90,316 |
|  |  |  |  |  |  | Mv | 29,321 |
| Height [mV] | 33.787 |  |  |  |  | Mp | 26,450 |
| Area [mV*s] | 3369.374 |  |  |  |  | Mz/Mw | 1.984 |
| Area% [%] | 7.010 |  |  |  |  | Mw/Mn | 2.469 |
| [eta] | 29320.69539 |  |  |  |  | Mz+1/Mw | 3.080 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 325 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.785 | 19.226 | 2,288 |  |  | Mw | 686 |
| Peak top | 12.265 | 37.577 | 518 |  |  | Mz | 1,128 |
| Peak end | 12.758 | 15.392 | 67 |  |  | Mz+1 | 1,460 |
|  |  |  |  |  |  | Mv | 686 |
| Height [mV] | 36.032 |  |  |  |  | Mp | 604 |
| Area [mV*s] | 1509.181 |  |  |  |  | Mz/Mw | 1.645 |
| Area% [%] | 3.140 |  |  |  |  | Mw/Mn | 2.110 |
| [eta] | 685.86396 |  |  |  |  | Mz+1/Mw | 2.129 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.758 | 15.392 | 67 |  |  | Mw | 5 |
| Peak top | 13.077 | 1000.000 | 12 |  |  | Mz | 12 |
| Peak end | 15.095 | 1.694 | 1 |  |  | Mz+1 | 21 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 998.412 |  |  |  |  | Mp | 13 |
| Area [mV*s] | 43189.685 |  |  |  |  | Mz/Mw | 2.520 |
| Area% [%] | 89.851 |  |  |  |  | Mw/Mn | 2.660 |
| [eta] | 4.88074 |  |  |  |  | Mz+1/Mw | 4.327 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 9.052 | 1.376 | 255,014 |  |  | Mw | 2,081 |
| Peak top | 13.077 | 1000.000 | 12 |  |  | Mz | 57,461 |
| Peak end | 15.095 | 1.694 | 1 |  |  | Mz+1 | 90,298 |
|  |  |  |  |  |  | Mv | 2,081 |
| Height [mV] | 1068.231 |  |  |  |  | Mp | 13 |
| Area [mV*s] | 48068.239 |  |  |  |  | Mz/Mw | 27.610 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1019.379 |
| [eta] | 2081.17212 |  |  |  |  | Mz+1/Mw | 43.388 |