Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/24 17:35:50 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EPE_unaged_2 |  |  |  |  |  |  | Calculation date and time | 2023/10/25 10:06:46 |
| Database name | SMF run-2023-10-24.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2389 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 8 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 13,674 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.818 | 1.614 | 385,129 |  |  | Mw | 37,648 |
| Peak top | 10.518 | 34.878 | 27,263 |  |  | Mz | 81,576 |
| Peak end | 11.765 | 18.074 | 2,412 |  |  | Mz+1 | 133,174 |
|  |  |  |  |  |  | Mv | 37,648 |
| Height [mV] | 33.260 |  |  |  |  | Mp | 31,980 |
| Area [mV*s] | 3581.706 |  |  |  |  | Mz/Mw | 2.167 |
| Area% [%] | 6.978 |  |  |  |  | Mw/Mn | 2.753 |
| [eta] | 37647.73390 |  |  |  |  | Mz+1/Mw | 3.537 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 330 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.765 | 18.074 | 2,412 |  |  | Mw | 700 |
| Peak top | 12.273 | 37.180 | 503 |  |  | Mz | 1,171 |
| Peak end | 12.745 | 17.549 | 71 |  |  | Mz+1 | 1,530 |
|  |  |  |  |  |  | Mv | 700 |
| Height [mV] | 35.559 |  |  |  |  | Mp | 615 |
| Area [mV*s] | 1499.955 |  |  |  |  | Mz/Mw | 1.672 |
| Area% [%] | 2.922 |  |  |  |  | Mw/Mn | 2.125 |
| [eta] | 700.36222 |  |  |  |  | Mz+1/Mw | 2.185 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.745 | 17.549 | 71 |  |  | Mw | 5 |
| Peak top | 13.038 | 1000.000 | 15 |  |  | Mz | 14 |
| Peak end | 15.068 | 1.627 | 1 |  |  | Mz+1 | 23 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 998.377 |  |  |  |  | Mp | 16 |
| Area [mV*s] | 46246.686 |  |  |  |  | Mz/Mw | 2.582 |
| Area% [%] | 90.100 |  |  |  |  | Mw/Mn | 2.911 |
| [eta] | 5.42418 |  |  |  |  | Mz+1/Mw | 4.266 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.818 | 1.614 | 385,129 |  |  | Mw | 2,652 |
| Peak top | 13.038 | 1000.000 | 15 |  |  | Mz | 80,805 |
| Peak end | 15.068 | 1.627 | 1 |  |  | Mz+1 | 133,159 |
|  |  |  |  |  |  | Mv | 2,652 |
| Height [mV] | 1067.197 |  |  |  |  | Mp | 16 |
| Area [mV*s] | 51328.346 |  |  |  |  | Mz/Mw | 30.465 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1282.713 |
| [eta] | 2652.42273 |  |  |  |  | Mz+1/Mw | 50.203 |