Chromatogram report

Header

| Title |  |  |  |  |  |  |  | Data acquisition date and time | 2023/10/24 17:55:50 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample name | EPE_unaged_3 |  |  |  |  |  |  | Calculation date and time | 2023/10/25 10:06:51 |
| Database name | SMF run-2023-10-24.chd |  |  |  |  |  |  | Acquisition time [min] | 0.500 - 20.000 |
| Data name | SMF2390 |  |  |  |  |  |  | Sampling interval [ms] | 100 |
| Method name | 03242023 |  |  |  |  |  |  | Cup number | 9 |
| Channel | RI |  |  |  |  |  |  | Calculation type | Molecular Mass |

Molecular mass calculation result (RI)

Peak 1 Base Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 12,584 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.883 | 1.155 | 342,580 |  |  | Mw | 34,126 |
| Peak top | 10.612 | 42.946 | 23,642 |  |  | Mz | 72,404 |
| Peak end | 11.795 | 22.114 | 2,227 |  |  | Mz+1 | 116,755 |
|  |  |  |  |  |  | Mv | 34,126 |
| Height [mV] | 41.798 |  |  |  |  | Mp | 29,028 |
| Area [mV*s] | 4398.525 |  |  |  |  | Mz/Mw | 2.122 |
| Area% [%] | 9.192 |  |  |  |  | Mw/Mn | 2.712 |
| [eta] | 34125.59558 |  |  |  |  | Mz+1/Mw | 3.421 |

Peak 2 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 328 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 11.795 | 22.114 | 2,227 |  |  | Mw | 697 |
| Peak top | 12.253 | 38.857 | 540 |  |  | Mz | 1,129 |
| Peak end | 12.775 | 12.656 | 62 |  |  | Mz+1 | 1,443 |
|  |  |  |  |  |  | Mv | 697 |
| Height [mV] | 37.716 |  |  |  |  | Mp | 629 |
| Area [mV*s] | 1596.479 |  |  |  |  | Mz/Mw | 1.620 |
| Area% [%] | 3.336 |  |  |  |  | Mw/Mn | 2.122 |
| [eta] | 696.75038 |  |  |  |  | Mz+1/Mw | 2.071 |

Peak 3 Valley Peak

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 12.775 | 12.656 | 62 |  |  | Mw | 5 |
| Peak top | 13.582 | 1000.000 | 1 |  |  | Mz | 11 |
| Peak end | 15.063 | 1.130 | 1 |  |  | Mz+1 | 19 |
|  |  |  |  |  |  | Mv | 5 |
| Height [mV] | 998.864 |  |  |  |  | Mp | 12 |
| Area [mV*s] | 41857.496 |  |  |  |  | Mz/Mw | 2.449 |
| Area% [%] | 87.472 |  |  |  |  | Mw/Mn | 2.550 |
| [eta] | 4.64812 |  |  |  |  | Mz+1/Mw | 4.140 |

Molecular mass calculation result (RI)

Total

|  | [min] | [mV] | [mol] |  |  | Mn | 2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Peak start | 8.883 | 1.155 | 342,580 |  |  | Mw | 3,164 |
| Peak top | 13.582 | 1000.000 | 1 |  |  | Mz | 71,787 |
| Peak end | 15.063 | 1.130 | 1 |  |  | Mz+1 | 116,742 |
|  |  |  |  |  |  | Mv | 3,164 |
| Height [mV] | 1078.378 |  |  |  |  | Mp | 12 |
| Area [mV*s] | 47852.499 |  |  |  |  | Mz/Mw | 22.688 |
| Area% [%] | 100.000 |  |  |  |  | Mw/Mn | 1519.006 |
| [eta] | 3164.08106 |  |  |  |  | Mz+1/Mw | 36.896 |